SHEN ZHEN SUMMER ELECTRONIC MATERIAL．LTD

Photosensitive ink line

(XR-777)

XR-777 Two-contact exposure for the development of anti-alkali etching, antioxidant, anti-plating ink for metal, glass, crystal, marble, jade and other materials to produce high precision on a variety of color patterns. After hardening at high temperature coating with good adhesion and high hardness and high gloss. It has anti-etching, plating resistance, anti-oxidation properties。

# 一、Feature

| Item | XR-S777 |
| --- | --- |
| Exterior | Main agent | Green, red, black, white, blue, yellow, purple liquid viscosity |
|  | Hardener | White turbid viscous liquid |
| Proportion（20℃） | Main agent | 1.1±0.01 |
|  | Hardener | 1.1±0.01 |
| Viscosity（25℃、VT-04 Type） | Main agent | 200±20PS |
|  | Hardener | 180±20PS |
|  | Mixed | 170±20PS |
| Hardener | 6H(Pencil hardness) |
| Light | 76℃ |
| Non-volatile components | 72wt% |
| Mixing ratio | Main agent 750g：Hardener 250g |
| Storage period | Main agent、Hardener | 6 months（25℃） |
|  | Two liquid mixture | 24 hours（25℃） |
| Printing area（1㎏） | About 16-20 square meters around |

# 二、Operational processes

Substrate pre-treatment

Acid treatment and brushing with the same general pre-treatment

Surface coating

Screen printing: full printing, mesh with the 43T-51T; or coating                        thickness 15-20U (India, for 15 minutes after spraying)

Pre-bake drying

75-85 ℃ ,30-40Minute

Exposure

# 1,350-450mj / cm, 21 light ladder Table 9-11 level (green, red, yellow, blue,           white) 2,650-700 mj / cm, 21 light ladder Table 12 (Black)   (1, 2 are for 15        minutes after exposure)

Significant impact

1-１.2 wt% Na2CO3，30±2℃，35-50S，Water pressure 2㎏/㎝

.

After hardening

1、(Green, red, yellow, blue, white) 150 ℃ -160 ℃ 60     minutes

2、Black in three stages: 100 ℃ 20 Minute

120 ℃ 40 Minute
                                         150℃-160℃            60 Minute

Blast: emery or aluminum oxide, sand thickness according to process requirements, the nozzle and work

In addition to film

15-20 cm from the surface of the etching: etching acid etching solution or alkaline solution oxidation: oxidation process requirements for general

Drawing: for valuables in the metal surface with a round wire or hemp for the drawing process

Sodium hydroxide solution. Concentration of 20-30%; temperature :45-65 ℃

# Note: Printed on both sides and then baked, is 70-75 ℃ ,40-50 Minute

# Third, note：

# 1, before using the main agent and hardener according to 750g: 250g weight ratio mixture, stir for 15 minutes after use, the mixture should be used within 24 hours.

# 2, the mixing method: First hardener mix, then take the 30g-40g hardener added to the main agent in Stir, then hardening agent added to the main agent, stir before using.

# 3, try not to add diluent, if diluted, the company with a thinner, less than 3% addition level.

# 4, the physical characteristics

| Item | Performance | Test Method (test conditions) |
| --- | --- | --- |
| Coating hardness | 6H Above | IPC-SM-840B 3.5.1.2 IPC-TM-650 2.4.27.2 |
| Abrasion resistance | OK | IPC-SM-840B 3.5.1.1 IPC-TM-650 2.4.27.1 Taber (3.5.1.1) Test Method: TM2.4.27.1 0.001 50 shall not be worn film |
| Adhesion | 100/100 OK | IPC-840B 3.5.2.1 TM 2.4.28.1 bottom of the metal and Hard floor (3.5.2.1) Test Method: Manual TM2.4.28 |
| Cutting | OK | IPC-840 3.5.3 To drilling, sawing or punching processing, etc., with visual inspection |
| Flammability | UL-94V-O | IPC-SM-840B 3.6.4 |

五、Chemical

| Project | Performance | Test Method (test conditions)） |
| --- | --- | --- |
| Solvent resistance | OK | IPC-SM 840B 3.6.1 No expansion on the film, peeling, color change is better Isopropyl alcohol Room temperature 60 Minute 1.1.1 Trichloroethane Room temperature 60 Minute ACETONE Room temperature 60 Minute Toluene Room temperature 60 Minute 10vo1% Sulfuric acid Room temperature 30 Minute 10vo1% Hydrochloric acid Room temperature 30 Minute 10wt% sodium hydroxide Room temperature 60 Minute |
| Decomposition of water-resistant | OK | IPC-SM-840 3.6.2 |
| Pressure cooker | OK | 120℃ 2 Barometric pressure 5 Hour |
| Resistance of gold | OK |  |

ADD：Shangshuijing Commercial Building No.B03# 10th Floor Buji Street of Shenzhen

TEL：0755-28545077  28545831  13509621917

FAX：0755-28545830